GENERAL PROCEDURE

for

ULTRASONIC THICKNESS MEASUREMENT

| DOCUMENT NUMBER: | IQMS-wT-P-001 |
| --- | --- |
| REVISION: | 00 |
| DOCUMENT DATE: | 21 JUNE 2017 |

18 Greybeard Road, Sandrift-North, Milnerton, 7441

Tel / Fax: +27(0) 21 555 2973   Mobile: +27(0) 79 957 2869

Email: cpt@iqms.co.za  Website: www.iqms.co.za

18 Greybeard Road, Sandrift-North, Milnerton, 7441

Tel / Fax: +27(0) 21 555 2973   Mobile: +27(0) 79 957 2869

Email: cpt@iqms.co.za  Website: www.iqms.co.za

Contents

1.	PURPOSE	3

2.	SCOPE	3

3.	DEFINITIONS AND ABBREVIATIONS	3

4.	NORMATIVE REFERENCES	3

5.	REQUIREMENTS	4

5.1	Personnel	4

5.2	Equipment	4

5.3	Transducers	4

5.4	Calibration	4

5.5	Couplants	4

5.6	Surface Conditions	5

5.7	Measurement of thicknesses	5

5.8	Reporting	5

APPENDIX A (Extract from SE-797)	6

PLEASE NOTE

This Document replaces all previous discussions, understandings and revisions of this written procedure for Ultrasonic Thickness Measurement utilized by IQMS Group.

PLEASE NOTE

This Document replaces all previous discussions, understandings and revisions of this written procedure for Ultrasonic Thickness Measurement utilized by IQMS Group.

# PURPOSE

This procedure encompasses the ultrasonic thickness measurement of materials, and is applicable to marine, aviation and general engineering needs for measuring depth of corrosion and establishing material thicknesses, to be used in the absence of a customer’s specific written procedure.

# SCOPE

Applicable to all butt welds in plate and pipe, castings and forgings when the Procedure Code is:

| ASME V, ART 23 (SE 797) | ASME Boiler and Pressure Vessel Code, Section V: Non-Destructive Examination |
| --- | --- |
| SNT-TC-1A | ASNT: Personnel qualification and certification in non-destructive testing |

(NB: The applicable version and addendum of the procedure code shall be stipulated by the client, AND a working copy may be requested by the Company from the client prior to conducting work under this procedure.)

Standard operating parameters of the Company shall be stipulated within each division.

# DEFINITIONS AND ABBREVIATIONS

| NDT | Non-Destructive Testing |
| --- | --- |
| UTM | ULTRASONIC THICKNESS MEASUREMENT |
| Technique Sheet | A document compiled, when required, in accordance with the Procedure Code detailing special instructions on equipment use and other information that will assist the Technician during the use of a Specialized Technique. |
| Technician (Operator) | An authorized Level I, II or III Technician authorized by the Company in accordance with IQMS-WP-001. |
| The Company | IQMS GROUP |
| Specialized Technique | Any UTM Technique not covered in this Procedure. |

# NORMATIVE REFERENCES

| IQMS-WP-001 | Written Practice for the Qualification, Internal Certification and Authorization of NDT Personnel. |
| --- | --- |
| IQMS-WP-002 | Written Practice for the Performance of NDT Equipment. |

# REQUIREMENTS

## Personnel

All personnel performing ultrasonic thickness gauging shall be authorized in accordance with IQMS-WP-001.

## Equipment

- The thickness monitoring equipment shall utilize the pulse-echo method and may be of digital or CRT/graphic display types, or digital and CRT/graphic combined.

- The equipment may either be set to a fixed material sound velocity or adjustable through a range of velocities.

- Some equipment is designed to enable thickness measurement to be made through paint or other coatings without the necessity of coating removal.

N.B. The coatings must be well bonded to the base material; otherwise measurement may not be possible.

## Transducers

- Transducer units (probes) may be of either single element or twin-element construction as provided with or compatible with the instrument. Generated sound frequencies shall be not lower than 2 Megahertz for thickness measurement of rolled or wrought steels.

- For most applications frequencies of 4 to 5 Megahertz are to be preferred, however if thicknesses less than ± 1 mm are to be measured frequencies up to as high as 10 Megahertz should provide more accurate results.

## Calibration

- For single transducer probe operation, a minimum of two thickness readings from known material thicknesses shall be displayed either simultaneously or consecutively. A delay adjustment control shall be incorporated into equipment utilizing single transducer probes with delay lines.

- For twin transducer probes a minimum of two thickness readings shall be displayed preferably consecutively, from a minimum of two known material thicknesses which encompass the highest and lowest thicknesses expected. This is necessitated by the parallax (vee-path) error which becomes significant when measuring thicknesses less than approximately 10mm.

- Calibration blocks shall be manufactured from material having the same sound velocity and attenuation as the material to be measured if possible, however if calibration is performed on blocks having a different sound velocity from the material to be measured, actual material measurements shall be multiplied by a correction factor calculated as follows: -

Actual Thickness=Measured thickness x Sound velocity in test materialSound velocity in calibration blocks

- The instrument operating manual should be followed closely until thoroughly familiar with the particular instrument.

## Couplants

- Any suitable liquid, oil or grease may be used, wall paper paste being probably the most popular.

- The couplant used shall not be deleterious to the surface or condition of the test material.

- The test material surface temperature shall not exceed 930C (2000 F).

## Surface Conditions

- Test surfaces shall be free from dust, rust, scale, paint etc., on rough, pitted or corroded test surfaces, a CRT or other graphic display is recommended.

- Materials at surface temperatures up to approximately 5400 C (10000 F) may be measured with specialized equipment and couplant, but at elevated temperatures over-reading is likely to occur by about 1% for each 550C (1000F).

Thus: -	if the instrument was calibrated on similar material at 200C (680 F) and the actual readings were taken at 4600 C (8600 F) the apparent thickness readings should be reduced by 8%.

## Measurement of thicknesses

- Poor coupling and rough or badly prepared surfaces may prevent digital displays from providing steady readings. If this occurs and cannot be rectified, a re-inspection using a graphic display instrument should be used.

- When coupling to hot surfaces, the couplant should be applied to the probe face, not to the hot surfaces, before coupling. Coupling for more than ± 3 seconds may raise the transducer element to a temperature which causes some depolarization to take place.

- Whilst ultrasonic thickness measurement generally consists of spot checking in specific areas, where required, scanning fully over a particular area may be necessary and should be performed at a speed not exceeding 150mm (6”) per second.

- When scanning fully, each line pass of the transducer shall overlap the previous pass by 10% of the transducer diameter or more.

- Digital display thickness readings shall be accurate to ± 0,1mm, whilst CRT/Graphic displays shall show discrimination of ± 1/4 of an individual time base scale division, i.e. 1/200 of calibrated sweep range.

- Each instrument shall be re-calibrated at intervals of no greater than 14 months by an NCS approved calibration facility.

- The re-calibration shall be supported with a calibration certificate and instrument label showing: -

- Re-calibration date

- Calibration facility name

- Validity period of the re-calibration

- The time base linearity of the instrument.

- Serial number and type of instrument

## Reporting

The following shall be recorded and included in each report as a minimum:

- Inspection procedure and reference number

- Type of instrument and serial number

- Calibration block materials and sound velocity

- Size, frequency and type of probe

- Scanning and/or spot checking method as appropriate

- Results

- Maximum and minimum thicknesses obtained

- Location map of measurements if required by client or agent

- Test personnel - Certification Level

# APPENDIX A (Extract from SE-797)

END.